|  | DYNAFLAIR CORPORATION 8147 Eagle Palm Drive Riverview, Florida 33569 Phone: 813-247-4770 Fax: 813-248-0900 |
| --- | --- |

# Aluminum Shutter Specification

| Shutter Slat Material: roll formed aluminum Slat Height: 44mm Paint: powder coat application of polyurethanic lacquer Standard Color: #25 white Foam Fill: expanded polyurethane, low density Maximum Width: 16 Ft. Maximum Height: 11 Ft. Weight (Slats Only): .61 lbs. per square foot |  |
| --- | --- |
| Box & End Plates Sizes: 7”X7” - for Shutters up to 7’0” max. ht. to top of end plate 8”X8” - for Shutters up to 9’0” max. ht. to top of end plate 10”X10” -for Shutters up to 11’0” max. ht. to top of plate Box Material: roll formed aluminum Paint: powder coat application of polyurethanic lacquer Standard Color: #25 white | Operator Option: Hand Crank - (available on shutters under 12ft. wide x 7ft. high) Electric Motor Note: 55 lb. limit for Hand Crank operated shutter |
| Guides Guide Material: extruded aluminum Size: 2-1/2”X7/8” Paint: powder coat application of polyurethanic laquer Standard Color: #25 white Liner: felt strip | Switch for Electric Operators: Wall Plate Style: Decora Color: white Type: rocker, 3 Position |

PANEL WEIGHT:  60 LBS. PER 3ft wide X6 ft. high panel assembled.